Date of issue:

Issued by:

# UnoBat 45 batten System                   6 pages

# NBS SPECIFICATION K21 CLAUSE 130

Project:				•

# BATTENED TIMBER FLOORING FLOATING FLOOR

Location:				•

Base and Preparation:	• New Existing (Delete as  necessary)  screed sub floor conforming to BS8204 Part 1 2003, to be flatness tolerance SR1, the surface of which should not deviate more than a 3mm gap showing under a 2m straight edge having a suitable damp proof membrane underneath.

•If block and beam suspended ground floor construction, ensure that the void is correctly ventilated to current Building Regulations with any earth base at least 225mm below any pre cast beams.

• As clause 260.

Surface Moisture Barrier	To screed lay Junckers Sylvathene moisture barrier with joints lapped and taped with waterproof tape and membrane turned up at the walls.

Batten System:	• Junckers UnoBat 45 veneer laminated spruce       batten system, 3.6m long incorporating resilient rubber shock absorbing strips.

•Finished size - 23mm deep x 45mm wide. Loose laid at 411mm centres with ends of alternate rows of battens staggered by at least 600mm and laid end to end.

All complying with EN 14904:2006, category A4.

• Load bearing capacity 5.0kN/m2. For information on retractable seating loadings contact Junckers.

• As clause 325.

Thermal Insulation		• If required.

between Battens

Boards:	• Junckers BREEAM A+ rated Solid Pre-finished hardwood, free from decay and insect attack and PEFC certified.  Planed all round. Comprising two rows of staves, with unique double dovetail construction.

•Polyback, polythene or lacquer moisture balancer fitted to the underside

Manufacturer:                              • Junckers Ltd

Tel No 0044 1376 534737

E mail sales@junckers.co.uk

Web www.junckers.co.uk

Area manager contact – ........................

Tel No .............................

Species:		•  Junckers Solid press dried European Beech

Grade:		• Classic, Premium or Club Grade (Delete as  necessary)

Finished Face Width:		•    129mm.

Finished Thickness:		•      22mm.

Finished Length:		•  3700mm.

Edges:	• Tongue and grooved.  Square edged and wax edged sealed.

Moisture Content		• 7.5% + manufacturing tolerance.

at Time of Fixing:

Fixing:	•  By secret nailing using 38mm lost head nails or 38mm machine nails or 38mm x 2.5mm diameter Pneumatic nails to each batten to each batten using a modified MAX pneumatic nail gun or equal and approved.

• Floor to be installed to a 10 board measure using Junckers PVC spacers, to suit the expected relative humidity range of the building when in use.

• 10 board measure to be …..............cm

• All laid to manufacturer’s recommendations.

• As clause 350.

Finish:                                  	• Factory finished with several coats of UV

light cured lacquer and one coat of Junckers

two-component polyurethane Isolacquer,

total film thickness 45 microns

Accessories:	• Junckers 38mm x 48mm Combi Skirting

boards.

• Junckers Bushings at post hole locations

Other Requirements:	           • Line marking to be carried out using Junckers

HP Sport Linemarking paint.

• One site applied coat of Junckers HP800 Sport lacquer on completion of line marking.

.

210		 WORKMANSHIP GENERALLY:

• Keep boards dry before installation.

• Methods of fixing and fasteners to be as section Z20 unless specified otherwise.

• Protect from dirt, stains and damage until Practical Completion using suitable coverings and boards laid as the work proceeds.

220				           ENVIRONMENT

• Do not start work specified in this section before building is weather tight, wet trades have finished their work and the building is fully dried out.

• Before, during and after installation, temperature and humidity must be maintained at levels approximating to those which will prevail after building is occupied.

• Relative humidity must be maintained within the range of 35-65%RH. This must be provided prior to installation and maintained from there on.

Exchange of Information

Ensure that there is a system in place for proper exchange of information between the design team and all specialist contractors, including persons responsible for commissioning and hand over, to ensure that the correct environmental conditions are achieved and maintained.

- HEATING

• Agree arrangements for operating the heating installation up to the date of Practical Completion of the Works to ensure that excessive moisture movement of flooring does not take place.

• The heating system has been designed to provide air temperatures in the range …………...°C  to……………ºC.

- FIXTURES:                                                     Do not start work specified in this section until any fixtures around which flooring is to be fixed have been installed.

- MOISTURE CONTENT OF BASE:  Where flooring is to be laid on a new or existing concrete or screed base:

• Ensure that drying aids have been turned off for not less than 4 days, then

• Test for moisture content using an accurately calibrated hygrometer in accordance with BS8201, Appendix A.

• Take readings in all corners, along edges, and at various points over the area being tested.

• Do not lay flooring until all readings show 75% RH or less.

- MOISTURE CONTENT OF TIMBER:       When instructed by CA, test timber with an approved moisture meter to manufacturer’s recommendations. Provide CA with records all tests and results.

290 		CONTROL SAMPLE:

Complete sample area, being part of the finished work, in approved location as follows and obtain approval of appearance before proceeding:

Clause reference:……………………..

Location:………………………………

Size:……………………………………

Include features:………………………

- FLOORING BATTENS

• Free from decay and active insect attack, and with no knots wider than half the width of the section.

• Veneer laminated spruce

• Moisture content 12-14%.

- FIXING BOARDS

• Fix each board securely to give a flat true surface free from undulations, hammer marks, scratches and protruding fastenings.

• Allow for movement of timber through expansion or contraction by installing to manufacturer’s recommendations to suit the expected relative humidity range of building when in use.

• Header joints to be tongue and grooved, tightly butted and positioned centrally over battens.

• Header joints to be uniformly positioned to an 822mm staggered pattern across the floor.

• Unless otherwise instructed surface nail first and last rows of boards.  Punch nails below surface and stop with filler, as recommended by flooring manufacturer.

- EXPANSION PROVISION

• Expansion gaps:

• Edges of flooring: Parallel to lie of boards form a clear perimeter gap equivalent to 1.5mm per running metre width of flooring on both sides and around pipes, columns etc. minimum size 15mm and to be covered by Junckers Combi Skirting 38mm x 48mm

• Ends of flooring: An expansion gap equivalent to 1mm per running metre length of flooring to be left at both ends of the floor.

• Intermediate expansion joints: Floor to be installed to a 10 board measure of      cm, using Junckers PVC spacers between every board.

• Remove any temporary spacer blocks and debris before fixing skirting/cover fillets.

.