Date of issue:

# Issued by:

# UnoBat 62+ System                  6 pages

# NBS SPECIFICATION K21 CLAUSE 130

Project:				•

# BATTENED TIMBER FLOORING FLOATING FLOOR

### Location:				•

Base and Preparation:	• New or (Delete as necessary) existing concrete base to comply with BS8204 Part 1 2003, to be flatness tolerance SR3, with a smooth, steel trowelled or wood float finish or better, with no surface irregularities or uneven undulations. Maximum permissible departure from the underside of a 2m straight edge resting in contact with the surface to be 10mm. (Use J Lock Wedge) Or –(delete as necessary)

New or (delete as necessary) existing screed base to comply with BS8204 Part 1 2003, to be flatness tolerance SR1, with a smooth, steel trowelled or wood float finish or better, with no surface irregularities or uneven undulations. Maximum permissible departure from the underside of a 2m straight edge resting in contact with the surface to be 3mm. (use J Lock)

All having a suitable damp proof membrane underneath

•If block and beam suspended ground floor construction, ensure that the void is correctly ventilated to current Building Regulations with any earth base at least 225mm below any precast beams.

• As clause 260.

Batten System:	•Junckers UnoBat 62+ veneer laminated spruce batten system.

• Finished size 26mm deep x 60mm wide by 3600mm long, mounted with rubber shock pads at 400mm centres each to be clicked into the Junckers “J Lock” shock elements or “J Lock Wedges” (delete as necessary).  Battens to be loose laid at 411mm centres with ends of alternate rows of battens staggered by at least 600mm and laid end to end. All ends of battens to have factory produced leaf joints.

Junckers Gable Battens to be installed as first and last rows at end walls.  All conforming to BS7044 Part 4, DIN 18032 Part 2 and BSEN14904:2006 Area A4

•Load bearing capacity 5.0kN/m2. For information on retractable seating loadings contact Junckers Ltd.

• All to be packed to a flatness tolerance of no more than a 3mm gap showing under a 2m straight edge.

Over all height of floor system including 22mm floor board –

- Using J Lock:	62mm or-

- Using J Lock Wedge and optional bases:

82mm to 209mm.

Ensure that any packing (if used) is securely fixed to the plastic “J Lock” or J Lock Wedge.

•  As clause 325.

Thermal Insulation		• If required.

#### between Battens

Moisture Membrane		• Junckers SylvaThene to be laid on top of the

cementitious base prior to installing the batten

system.

• As clause 310.

Boards:	• Junckers BREEAM A+ rated Solid Pre-finished hardwood, free from decay and insect attack and PEFC certified. Planed all round. Consisting of two rows of staves with unique double dovetail construction.

•Polyback, polythene or lacquer moisture balancer factory-applied to the underside of the floorboard.

Manufacturer:                              • Junckers Ltd

1 Wheaton Road, Witham, Essex, CM8 3UJ

Tel No 0044 1376 534737

E mail sales@junckers.co.uk

Web www.junckers.co.uk

Area manager contact – ........................

Tel No .............................

Species:		•   Junckers Solid press dried Beech

Grade:		• SylvaSport Premium or (Delete as necessary)

Club or (Delete as necessary) SylvaTech plus

Premium or (Delete as necessary) Club.

Finished Face Width:		•    129mm.

Finished Thickness:		•      22mm.

Finished Length:		•  3700mm.

Edges:	• Tongue and grooved.  Square edged and wax edged sealed.

Moisture Content		• 7.5% + manufacturing tolerance.

at Time of Fixing:

Fixing:	•  By secret nailing using 50mm – 65mm lost head nails or 2.5mm diameter Pneumatic nails to each batten to each batten using a modified MAX pneumatic nail gun.

• Floor to be installed to a 10 board measure, using Junckers PVC spacers to suit the expected relative humidity range of the building when in use.

• 10 Board measure to be………………

• All laid to manufacturer’s recommendations.

• As clause 350.

Finish:	            •  Factory finished with several coats of UV

light cured lacquer and one coat of Junckers

two-component polyurethane Isolacquer, total

film thickness 45 microns

Accessories:	• Junckers Combi Skirting 38mm x 48mm to be fixed to all walls.

• Junckers Bushings to be fitted at post socket locations.

Other Requirements:	           • Line marking to be carried out using Junckers

HP SportsLine paint.

• One coat of Junckers HP Sport lacquer to be applied on completion of line marking.

210	WORKMANSHIP GENERALLY:

•   Keep boards dry before installation.

• Methods of fixing and fasteners to be as section Z20 unless specified otherwise.

• Protect from dirt, stains and damage until Practical Completion using suitable coverings and boards laid as the work proceeds.

220				           ENVIRONMENT

• Do not start work specified in this section before building is weather tight, wet trades have finished their work and the building is fully dried out.

• Before, during and after installation, temperature and humidity must be maintained at levels to match those which will prevail after building is occupied.

• Relative humidity must be maintained within the range of 35-65%RH. This must be provided prior to installation and maintained from there on.

Exchange of Information

Ensure that there is a system in place for proper exchange of information between the design team and all specialist contractors, including persons responsible for commissioning and hand over, to ensure that the correct environmental conditions are achieved and maintained.

##### HEATING

• Agree arrangements for operating the heating installation up to the date of Practical Completion of the Works to ensure that excessive moisture movement of flooring does not take place.

• The heating system has been designed to provide air temperatures in the range …………...°C  to……………ºC.

- FIXTURES:                                                     Do not start work specified in this section until any fixtures around which flooring is to be fixed have been installed.

- MOISTURE CONTENT OF BASE:                Where flooring is to be laid on a new or existing concrete or screed base:

• Ensure that drying aids have been turned off for not less than 4 days, then

• Test for moisture content using an accurately calibrated hygrometer in accordance with BS8201, Appendix A.

•   Take readings in all corners, along edges, and at various points over the area being tested.

•   Do not lay flooring until all readings show 75% RH or less.

- MOISTURE CONTENT OF TIMBER:         When instructed by CA, test timber with an approved moisture meter to manufacturer’s recommendations. Provide CA with records all tests and results.

290 		CONTROL SAMPLE

Complete sample area, being part of the finished work, in approved location as follows and obtain approval of appearance before proceeding:

Clause reference:……………………..

Location:………………………………

Size:……………………………………

Include features:………………………

310		VAPOUR CHECK/MOISTURE MEMBRANE

• To be lapped, taped and turned up at perimeter walls.

• Ensure membrane is clean, dry and free from punctures and tears before laying flooring.

- FLOORING BATTENS

• Free from decay and active insect attack, and with no knots wider than half the width of the section.

• Veneer laminated spruce

• Moisture content 12-14%.

- FIXING BOARDS

• Fix each board securely to give a flat true surface free from undulations, hammer marks, scratches and protruding fastenings.

• Allow for movement of timber through expansion or contraction by installing to manufacturer’s recommendations to suit the expected relative humidity range of building when in use.

• Header joints to be tongue and grooved, tightly butted and positioned centrally over battens.

•   Header joints to be uniformly positioned to an 822mm staggered pattern across the floor.

• Unless otherwise instructed surface nail first and last rows of boards.  Punch nails below surface and stop with filler, as recommended by flooring manufacturer.

- EXPANSION PROVISION:

• Expansion gaps:

• Edges of flooring: Parallel to lie of boards form a clear perimeter gap equivalent to 1.5mm per running metre width of floor on both sides and around pipes, columns etc. minimum size 15mm and to be covered by Junckers Combi Skirting 38mm x 48mm.

• Ends of flooring: An expansion gap equivalent to 1mm per running metre length of floor to be left at both ends of the floor.

• Intermediate expansion joints: Floor to be installed to a 10 board measure of…………cm, using Junckers PVC spacers between boards.

• Remove any temporary spacer blocks and debris before fixing skirting/cover fillets.